Revealing the activity of different iron carbides for Fischer-Tropsch synthesis

Fangxu Lu, Xin Chen, Zhigang Lei, Lixiong Wen*, Yi Zhang*

College of Chemical Engineering, Beijing University of Chemical Technology, 15 Beisanhuan East Road, Beijing 100029, PR China

Figure S1. The XRD patterns of fresh catalysts.

Figure S2. XPS spectra of Fe 2p on the fresh catalysts.

Figure S3. N2 adsorption-desorption isotherms of the fresh α-Fe2O3 catalyst.

1 um

1 um

Figure S4 A) SEM-EDX elemental mapping of Fe and Al for the fresh Al2O3/α-Fe2O3=1 catalyst; B) SEM-EDX elemental mapping of Fe and Si for the fresh SiO2/α-Fe2O3=1 catalyst.

Figure S5 TEM images of the pure α-Fe2O3 catalyst before (A) and after (B) FTS reaction.

Figure S6 The CO-TPR profiles of various fresh catalysts for CO consumption.

Figure S7 CO-DRIFT spectrum of the Al2O3.

(b)

(a)

Figure S8 NH3-TPD (a) and CO2-TPD (b) of SiO2 and Al2O3.

Table S1. The results of in-situ XPS for Fe 2p 3/2

| catalysts | Binding energy (eV) Fe 2p3/2 |  |  |  | Iron carbide (atom%) Fe 2p3/2 |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Fe2C | Fe5C2 | Fe3C | Fe2O3 | Fe2C | Fe5C2 | Fe3C | Fe2O3 |
| α-Fe2O3 | 706.1 | 707.0 | 707.9 | 709.9 | 1.2 | 22.2 | 15.5 | 61.1 |
| SiO2/α-Fe2O3=1 | 706.7 | 707.3 | 708.3 | 710.4 | 7.1 | 19.3 | 11.7 | 61.9 |
| Al2O3/α-Fe2O3=1 | 706.7 | 707.2 | 708.2 | 710.2 | 13.2 | 18.0 | 10.3 | 58.5 |

Table S2. The location and content of linear adsorbed CO on different iron carbides from in-situ CO-DRIFT.

| catalysts | Wavenumber (cm-1) |  |  | Content of the adsorbed CO (%) |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Fe2C | Fe5C2 | Fe3C | Fe2C | Fe5C2 | Fe3C |
| α-Fe2O3 | - | 2013 | 2027 | - | 63.2 | 36.8 |
| SiO2/α-Fe2O3=1 | 2004 | 2014 | 2032 | 18.6 | 57.3 | 24.1 |
| Al2O3/α-Fe2O3=1 | 2006 | 2016 | 2033 | 27.7 | 49.3 | 23.0 |