Supplementary Material for

Study on CaO-promoted Co/AC catalysts for synthesis of higher alcohols from syngas

Hong Du,a,c Hejun Zhu,a* Xingkun Chen,a,c Wenda Dong,a Wei Lu,a Wenting Luo,a,c Miao Jiang,a,c Tao Liu, a Yunjie Ding a,b*

a Dalian National Laboratory for Clean Energy, Dalian Institute of Chemical Physics, Chinese Academy of Sciences, Dalian, 116023, China

b State Key Laboratory of catalysis, Dalian Institute of Chemical Physics, Chinese Academy of Sciences, Dalian, 116023, China

c University of Chinese Academy of Sciences, Beijing 100039, China

Figure S1. Pore size distribution curves of the AC support and corresponding catalysts calculated from non-local density functional theory (NLDFT).

Figure S2. XRD patterns for the spent 15Co0.5Ca/AC and 15Co0.5Ca/γ-Al2O3 catalysts.

Figure S3. Scheme of CO hydrogenation reaction pathway over the 15Co-xCa/AC catalysts.

Table S1 The performance of CO hydrogenation over the 15Co0.5Ca/AC and 15Co0.5Ca/γ-Al2O3 catalysts a

| Catalyst | CO Conversion /% | Selectivity/C % |  |  |  | Alcohol Yield, % | Alcohol distribution/wt % |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | HC1-4 b | CO2 | HC5+ c | ROH d |  | C1OH e | C2+OH f |
| 15Co0.5Ca/AC | 24.7 | 48.0 | 1.3 | 21.4 | 29.3 | 7.2 | 4.2 | 95.8 |
| 15Co0.5Ca/γ-Al2O3 | 16.5 | 56.9 | 0.6 | 34.1 | 8.4 | 1.4 | 6.2 | 93.8 |

a Reaction conditions: P = 3.0 MPa, T = 493 K, GHSV = 900 h-1.

b Hydrocarbons with carbon numbers of 1-4.

c Hydrocarbons with carbon numbers more than 4.

d Alcohols with carbon numbers of 1-18.

e CH3OH

f Alcohols with carbon numbers more than one..