Supporting Information

Highly active and controllable MOF-derived carbon nanosheets supported iron catalysts for Fischer-Tropsch synthesis

Qiao Zhaoa, Shouying Huanga,∗, Xiaoxue Hana, Jiajia Chena, Junhu Wangb, Alexandre Rykovb, Yue Wanga, Meiyan Wanga, Jing Lva, Xinbin Ma a,∗∗

aKey Laboratory for Green Chemical Technology of Ministry of Education Collaborative Innovation Center of Chemical Science and Engineering, School of Chemical Engineering and Technology, Tianjin University, Tianjin, 300072, China

bMössbauer Effect Data Center, Dalian Institute of Chemical Physics, Chinese Academy of Sciences, Dalian, 116023, China

∗Corresponding author.

∗∗Corresponding author.

Fig. S1. 57Fe Mössbauer spectra of the fresh Fe/AC, Fe/CP and Fe/CNS(1000) catalysts.

Table S1 57Fe Mössbauer parameters of the fresh Fe/AC, Fe/CP and Fe/CNS(1000) catalysts.

| Fresh catalysts | IS (mm·s-1) | QS (mm·s-1) | H (T) | Phase ascription | A (%) |
| --- | --- | --- | --- | --- | --- |
| Fe/AC | 0.32 | 0.70 | - | Fe(Ⅱ)/ Fe(Ⅲ) | 97.2 |
|  | 0.17 | 0.03 | 18.0 | χ-Fe5C2(A) | 1.1 |
|  | 0.22 | 0.09 | 21.6 | χ-Fe5C2(B) | 1.1 |
|  | 0.20 | 0.11 | 11.1 | χ-Fe5C2(C) | 0.6 |
| Fe/CP | 0.33 | 0.72 | - | Fe(Ⅱ)/ Fe(Ⅲ) | 89.8 |
|  | 0.17 | 0.03 | 18 | χ-Fe5C2(A) | 4.8 |
|  | 0.22 | 0.09 | 21.6 | χ-Fe5C2(B) | 4.8 |
|  | 0.20 | 0.11 | 11.1 | χ-Fe5C2(C) | 0.6 |
| Fe/CNS(1000) | 0.33 | 0.75 | - | Fe(Ⅱ)/ Fe(Ⅲ) | 90.5 |
|  | 0.17 | 0.03 | 18.0 | χ-Fe5C2(A) | 3.8 |
|  | 0.22 | 0.09 | 21.6 | χ-Fe5C2(B) | 3.8 |
|  | 0.20 | 0.11 | 10.9 | χ-Fe5C2(C) | 1.9 |

Fig. S2. TEM images of the Fe/CNS(1000) catalysts in dark field, and corresponding mappings of C, N, Fe and O.

Fig. S3. N2 adsorption-desorption isotherms (a, c) and pore size distribution (b, d) of the CNS(T), and corresponding iron-based catalysts.

Table S2 Surface area and pore structure parameters of CNS(T) and Fe/CNS(T) catalysts.

| samples | SBET (m2g-1) | Vtotal (cm3g-1) | Vmicro (cm3g-1) | Da (nm) |
| --- | --- | --- | --- | --- |
| CNS(900) | 272 | 0.12 | 0.10 | 1.7 |
| CNS(950) | 416 | 0.18 | 0.15 | 1.8 |
| CNS(1000) | 438 | 0.20 | 0.15 | 1.8 |
| CNS(1100) | 524 | 0.23 | 0.18 | 1.8 |
| Fe/CNS(900) | 194 | 0.12 | 0.06 | 2.3 |
| Fe/CNS(950) | 208 | 0.13 | 0.07 | 2.4 |
| Fe/CNS(1000) | 210 | 0.14 | 0.08 | 2.1 |
| Fe/CNS(1100) | 250 | 0.15 | 0.09 | 2.3 |

Table S3 FTS performance of Fe/CNS(T) catalysts at changeable space velocity.

| Catalysts | CO conv. (%) | FTY (μmolCO gFe-1s-1) | CO2 selectivity (%) | Hydrocarbon selectivity (C-mol%) |  |  |  |  | O/P |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | CH4 | C2-C4= | C2-C4o | C5+ | Oxy. |  |  |  |
| Fe/CNS(900) | 33.9 | 198 | 31.9 | 26.5 | 28.4 | 15.8 | 28.4 | 0.9 |  | 1.8 |  |
| Fe/CNS(950) | 34.9 | 278 | 30.5 | 27.2 | 26.3 | 15.3 | 30.4 | 0.8 |  | 1.7 |  |
| Fe/CNS(1000) | 34.7 | 323 | 31.6 | 27.5 | 24.9 | 15.6 | 31.2 | 0.8 |  | 1.6 |  |
| Fe/CNS(1100) | 31.2 | 191 | 28.6 | 28.4 | 23.0 | 16.3 | 31.6 | 0.7 |  | 1.4 |  |

Reaction conditions: 0.1 g cat., 340 °C, 1 MPa, H2/CO=1, GHSV=9000-14000 mL·g-1·h-1, TOS=30 h.

Fig. S4. CO conversion of Fe/CNS(T) catalysts on TOS. (P = 1 MPa, H2/CO = 1, GHSV = 9000 mL·g-1·h-1, T = 340 °C)

Fig. S5. TEM images of the used Fe/CNS(T) after 100 h reaction: Fe/CNS(900) (a), Fe/CNS(950) (b), Fe/CNS(1000) (c) and Fe/CNS(1100) (d) (diagrams below them are the iron particle size distribution of corresponding catalysts).

Fig. S6. HR-TEM images of the used Fe/CNS(1000).

Fig. S7. XRD patterns of the used Fe/CNS(1000), Fe/CP, Fe/AC.

Fig. S8. 57Fe Mössbauer spectra of the used Fe/CNS(900), Fe/CNS(1000) and Fe/CNS(1100) catalysts.