Supporting Information

Rational Design of Hierarchical Zeolite Encapsulating FeMnK Architecture to Enhance Light Olefins Selectivity in Fischer-Tropsch Synthesis

Can Zhu, 1,2 Chao Huang, 1,2 Mingwei Zhang, *,1 Yizhuo Han, 1 and Kegong Fang *,1

1 State Key Laboratory of Coal Conversion, Institute of Coal Chemistry, Chinese Academy of Sciences, Taiyuan 030001, Shanxi, People’s Republic of China

2 University of Chinese Academy of Sciences, Beijing 100049, People’s Republic of China

Corresponding Authors:

*E-mail for Mingwei Zhang: zmwsdust@126.com

*E-mail for Kegong Fang: kgfang@sxicc.ac.cn

Tables and Figures

Figure S1. The HAADF-STEM images and the results of EDX elemental (Fe, Mn, K, Si, O) mapping of FeMnK@H-S-1(0.10) catalyst

Table S1. Element content of FeMnK@H-S-1(x) catalysts.

| Catalyst | Fe (wt %)a | Mn (wt %)a | K (wt %)a | Na (wt %)a | Fe (wt %)b |
| --- | --- | --- | --- | --- | --- |
| FeMnK@H-S-1(0.00) | 8.17 | 4.21 | 0.65 | - | 1.12 |
| FeMnK@H-S-1(0.10) | 7.81 | 4.08 | 0.56 | 0.26 | 1.03 |
| FeMnK@H-S-1(0.20) | 8.22 | 4.12 | 0.55 | 1.19 | 1.03 |
| FeMnK@H-S-1(0.50) | 9.19 | 4.59 | 0.53 | 1.33 | 1.06 |
| FeMnK@H-S-1(0.67) | 8.45 | 4.14 | 0.59 | 1.09 | 1.44 |
| FeMnK@H-S-1(0.80) | 9.20 | 4.66 | 0.48 | 1.78 | 1.20 |

a Determined by XRF

b Determined by XPS

Table S2. Textural properties of FeMnK@H-S-1(x) catalysts

| Catalyst | SBETa (m2g-1) | Smicrob (m2g-1) | Smesoc (m2g-1) | Vmicrob (cm3g-1) | Vtotale (cm3g-1) | HF |
| --- | --- | --- | --- | --- | --- | --- |
| FeMnK@H-S-1(0.00) | 354.2 | 259.7 | 94.5 | 0.112 | 0.475 | 0.063 |
| FeMnK@H-S-1(0.10) | 321.1 | 218.5 | 102.6 | 0.096 | 0.471 | 0.065 |
| FeMnK@H-S-1(0.20) | 305.5 | 192.4 | 113.1 | 0.088 | 0.398 | 0.081 |
| FeMnK@H-S-1(0.50) | 300.4 | 209.6 | 90.8 | 0.092 | 0.376 | 0.074 |
| FeMnK@H-S-1(0.67) | 256.0 | 192.9 | 63.1 | 0.085 | 0.311 | 0.067 |
| FeMnK@H-S-1(0.80) | 216.2 | 156.8 | 59.4 | 0.071 | 0.283 | 0.069 |

a BET method.  b Measured by t-plot method.

c Mesoporous surface area: Smeso = SBET -Smicro.

e Single point pore volume obtained from N2 adsorbed at P/Po = 0.99.

Figure S2. XPS spectra of Si 2p on different FeMnK@H-S-1(x) catalysts.

Table S3. Catalytic performance of FeMnK/S-1 catalyst

| Catalyst | CO Conv. (%) | CO2 Sele. (%) | Hydrocarbon distribution (C%) |  |  |  | O/P |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | CH4 | C2=-C4= | C2o-C4o | C5+ |  |
| FeMnK/S-1 | 15.2 | 36.0 | 13.8 | 33.9 | 6.5 | 45.8 | 5.2 |

Reaction conditions: 280 oC, 0.5 MPa, 4000 h-1, H2/CO=1.90. m(catalyst)=0.85 g

Table S4. Catalytic performance of FeMnK+H-S-1 and FeMnK catalysts

| Catalyst | CO Conv. (%) | CO2 Sele. (%) | Hydrocarbon distribution (C%) |  |  |  | O/P |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | CH4 | C2=-C4= | C2o-C4o | C5+ |  |
| FeMnK+H-S-1 | 13.3 | 47.8 | 16.9 | 37.1 | 8.3 | 37.6 | 4.5 |
| FeMnK | 11.8 | 47.2 | 16.8 | 32.0 | 7.4 | 43.8 | 4.3 |

Reaction conditions: 280 oC, 0.5 MPa, 4000 h-1, H2/CO=1.90.

Table S5. Comparison of the results in literature works for CO Hydrogenation to light olefins of iron-based catalysts and our work.

| Catalyst | CO Conv.(%) | FTY µmolCO.gFe.-1.S-1 | CO2 Sele.(%) | Hydrocarbon distribution |  |  |  | STY µmolC2=-C4=.gFe-1.S-1 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | CH4 | C2=-C4= | C2o-C4o | C5+ |  |
| Fe/C@Si-SAPO·K1 | N.A. | 27.0 | 25.0 | 34.7 | 40.3 | 13.6 | 11.4 | N.A. |
| FeMnK/Al2O3@S22 | 4.0 | 28.0 | 25.1 | 42.7 | 38.1 | 15.6 | 3.4 | N.A. |
| Fe20-Mn1.0/SiO2 3 | 14.4 | N.A. | 23.3 | 21.6 | 32.3 | N.A. | 19.4 | N.A. |
| Fe/MnK-CNTs 4 | 22.7 | N.A. | N.A. | 28.8 | 50.3 | 7.6 | 13.3 | N.A. |
| Fe-Na-S/CNF 5 | N.A. | 26.8 | N.A. | 36.0 | 52.0 | 6.0 | 6.0 | N.A. |
| Fe-K/NCNTs 6 | 16.5 | 27.9 | 23.6 | 17.3 | 54.6 | 5.9 | 22.2 | N.A. |
| FeBi/CNT-in 7 | 25.6 | 47.0 | 37.3 | 27.0 | 62.4 | 6.5 | 4.6 | 18.4 |
| FePb/CNT-in 7 | 35.9 | 66.0 | 39.9 | 26.1 | 58.9 | 7.4 | 7.6 | 23.4. |
| This work 8 | 13.9 | 85.9 | 38.6 | 24.2 | 50.6 | 9.9 | 15.2 | 26.7 |

- Reaction conditions: 340 oC, 1.0 MPa, H2/CO = 1, 16 SL.gcat-1.h-1

- Reaction conditions: 340 °C, 2.0 MPa, H2/CO=1, WHSV=4500 mL.g-1·h-1

- Reaction conditions: 260 °C 2.0 MPa, H2/CO=1, GHSV=4000 h-1

- Reaction conditions: 270 °C 2.0 MPa, H2/CO=1, GHSV=30000mL. gcat-1.h-1

- Reaction conditions: 350 °C, 0.1 MPa, H2/CO = 1,

- Reaction conditions: 300 °C, 0.1 MPa, H2/CO = 1, WHSV=4200 mL.g-1·h-1

- Reaction conditions: 350 °C, 0.1 MPa, H2/CO = 1, GHSV=3.4L. gcat-1.h-1

- Reaction conditions: 280 °C, 0.5 MPa, H2/CO = 1.9, GHSV=4000 h-1

Figure S3. The space time yield (STY) of light olefins versus hierarchy factor.

Figure S4. C2H4-TPD-MS profile of reduced FeMnK oxide.

Table S6. Element content of Na modified FeMnK@H-S-1(0.00) catalyst derived from XRF

| Catalyst | Fe (wt %) | Mn (wt %) | K (wt %) | Na (wt %) |
| --- | --- | --- | --- | --- |
| FeMnK@H-S-1(0.00)-1.17Na | 7.49 | 3.60 | 0.69 | 1.17 |

Table S7. Catalytic performance of FeMnK@H-S-1(0.00) and Na modified FeMnK@H-S-1(0.00) catalysts

| Catalyst | CO Conv. (%) | CO2 Sele. (%) | Hydrocarbon distribution (C%) |  |  |  | O/P |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | CH4 | C2=-C4= | C2o-C4o | C5+ |  |
| FeMnK@H-S-1(0.00) | 7.5 | 16.2 | 33.5 | 31.8 | 29.4 | 5.3 | 1.1 |
| FeMnK@H-S-1(0.00) 1.17Na | 7.8 | 17.3 | 31.8 | 33.9 | 27.8 | 6.5 | 1.2 |

Reaction conditions: 280 oC, 0.5 MPa, 4000 h-1, H2/CO=1.90. m(catalyst)=0.85 g