# Supplementary Material

Promotional effect of Mn-doping on the structure and performance of spinel ferrite microspheres for CO hydrogenation

Bianfang Shia, #, Zhengpai Zhanga,#, Yitao Liua, Junjie Sua, Xianglin Liua, Xuning Lib,c, Junhu Wangb,d, Minghui Zhua, Zixu Yanga, Jing Xua,*, Yifan Hana,e,*

- State Key Laboratory of Chemical Engineering, East China University of Science and Technology, Shanghai 200237, China

- State Key Laboratory of Catalysis, Dalian Institute of Chemical Physics, Chinese Academy of Sciences, Dalian 116023, China

- School of Chemical and Biomedical Engineering, Nanyang Technological University, 62 Nanyang Drive, Singapore 637459, Singapore

- Mössbauer Effect Data Center, Dalian Institute of Chemical Physics, Chinese Academy of Sciences, Dalian 116023, China

- Engineering Research Center of Advanced Functional Material Manufacturing of Ministry of Education, Zhengzhou University, Zhengzhou 450001, China.

* Corresponding author phone: (+86) 021-64251928; Fax: (+86) 021-64253528;

Email: yifanhan@ecust.edu.cn; xujing@ecust.edu.cn

# Equal contribution

Contents

Table S1 Quantitative H2 consumption area of Fe-Mn microspheres during TPRa

Table S2 57Fe Mössbauer parameters of the spent Fe-Mn microspheres after FTO reactiona.

Table S3 Phase composition of the spent Fe-Mn microspheres from Mössbauer spectroscopy.

Table S4 FTO performance of Fe-Mn microspheres with different Mn contentsa.

Table S5 FTO performance at different H2/CO ratios in syngas over Fe-13Mn catalysta.

Table S6 FTO performance during a temperature-scanning experiment at temperatures ranging from 493-613 K over Fe-13Mn catalysta.

Fig. S1. Total area of H2 consumption as a function of Mn loading from TPR experiments

Fig. S2. Iron-time-yield (FTY), product distribution and C2=-C4= olefin space-time-yield (STY) at different H2/CO ratios (0.5, 1, 3) in syngas over a Fe-13Mn catalyst. Reaction conditions: 25mg catalyst diluted with SiC (1:3), 533K, 2.0 MPa, GHSV=4000 h-1, TOS= 20h, syngas composition (%, v/v, H2/CO/N2) = 30/60/10, 45/45/10, 60/20/20.

Fig. S3. Iron-time-yield (FTY), product distribution and C2=-C4= olefin space-time-yield (STY) during a temperature-scanning experiment in the range 493-613K over a Fe-13Mn catalyst. Reaction conditions: 25mg catalyst diluted with SiC (1:3), 2.0 MPa, GHSV=4000 h-1, TOS= 20h, H2/CO=1.

Table S1

Quantitative H2 consumption area of Fe-Mn microspheres during TPRa

| Catalyst | Expected H2 Consumption Area (x107, a.u.) | Actual H2 Consumption Area (x107, a.u.) | Reduction Degree (%) |
| --- | --- | --- | --- |
| Fe-0Mn | 1.680 | 1.680 | 100 |
| Fe-2Mn | 1.647 | 1.646 | 99.9 |
| Fe-13Mn | 1.464 | 1.306 | 89.2 |
| Fe-31Mn | 1.163 | 0.545 | 46.9 |

a Assume that Fe-0Mn composed of Fe3O4 can be fully reduced to metallic Fe during the TPR, and no reduction of divalent Mn is involved for all the catalysts.

Table S2

57Fe Mössbauer parameters of the spent Fe-Mn microspheres after FTO reactiona.

| Spent catalysts | Phases | IS/mm s-1 b | QS/mm s-1 c | Hhf/ kOe d | Area % e |
| --- | --- | --- | --- | --- | --- |
| Fe-0Mn | Fe3O4 (A) | 0.28 | 0.00 | 497 | 10.8 |
|  | Fe3O4 (B) | 0.67 | -0.01 | 464 | 21.5 |
|  | χ-Fe5C2 (I) | 0.24 | 0.12 | 216 | 27.1 |
|  | χ-Fe5C2 (II) | 0.20 | 0.07 | 109 | 16.2 |
|  | ε-Fe2C | 0.17 | 0.07 | 187 | 24.4 |
| Fe-13Mn | Fe3O4 (B) | 0.42 | 0.07 | 464 | 16.4 |
|  | Fe3+ (spm) | 0.28 | 1.03 | - | 9.5 |
|  | χ-Fe5C2 (I) | 0.24 | 0.12 | 217 | 24.3 |
|  | χ-Fe5C2 (II) | 0.22 | 0.03 | 111 | 16.9 |
|  | ε-Fe2C | 0.17 | 0.05 | 187 | 33.0 |
| Fe-31Mn | Fe3+ (spm) | 0.29 | 0.72 | - | 22.5 |
|  | Fe2+ (spm) | 1.09 | 0.51 | - | 34.2 |
|  | χ-Fe5C2 (I) | 0.26 | 0.12 | 213 | 12.1 |
|  | ε-Fe2C | 0.23 | 0.06 | 176 | 31.2 |

a Reaction conditions: H2/CO=1.0, 533 K, 2.0 MPa and 4000 h-1; b isomer shift; c quadruple splitting; d Hyperfine magnetic field; e relative absorption area.

Table S3

Phase composition of the spent Fe-Mn microspheres from Mössbauer spectroscopy.

| Spent catalysts | Total oxides, % | Total carbides, % | ε-Fe2C, % | χ-Fe5C2, % | ε-Fe2C/χ-Fe5C2 ratio |
| --- | --- | --- | --- | --- | --- |
| Fe-0Mn | 32.3 | 67.7 | 24.4 | 43.3 | 0.56 |
| Fe-13Mn | 25.8 | 74.2 | 33.0 | 41.2 | 0.80 |
| Fe-31Mn | 56.7 | 43.3 | 31.2 | 12.1 | 2.58 |

Table S4

FTO performance of Fe-Mn microspheres with different Mn contentsa.

| Catalysts | CO conv., % | CO2 sel., % | Hydrocarbon distribution, carbon based, mol %b |  |  |  |  |  |  |  |  |  | FTYc, molCO·gFe-1·s-1 | C2-4= STYd, g·kgcat-1·h-1 | O/Pe ratio |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | CH4 | C2= | C3= | C4= | C2-4= | C20 | C30 | C40 | C2-40 | C5+ |  |  |  |
| Fe-0Mn | 6.2 | 16.7 | 20.7 | 6.5 | 18.7 | 7.8 | 33.0 | 11.3 | 5.2 | 11.0 | 27.6 | 18.7 | 14.3 | 42.9 | 1.2 |
| Fe-2Mn | 5.6 | 19.2 | 18.6 | 9.2 | 22.6 | 10.5 | 42.4 | 10.9 | 5.8 | 9.7 | 26.4 | 12.6 | 12.8 | 48.5 | 1.6 |
| Fe-13Mn | 7.1 | 25.2 | 17.0 | 13.6 | 25.2 | 15.6 | 54.4 | 6.0 | 4.1 | 5.1 | 15.2 | 13.3 | 16.9 | 73.0 | 3.6 |
| Fe-31Mn | 3.3 | 17.8 | 22.4 | 12.7 | 24.0 | 13.1 | 49.8 | 6.4 | 4.2 | 6.2 | 16.8 | 11.0 | 10.9 | 34.2 | 3.0 |

a Reaction conditions: 25mg catalyst diluted with SiC (1:3), 533K, 2.0 MPa, H2/CO=1, GHSV=4000h-1, TOS= 20h. b The hydrocarbon distribution is normalized on a carbon basis with the exclusion of CO2. c Iron time yield (FTY) = mol of CO converted to hydrocarbons (excluding CO2) per time (s) per weight of iron (g). d STY = space time yield. e olefin/paraffin ratio of C2-4 hydrocarbons.

Table S5

FTO performance at different H2/CO ratios in syngas over Fe-13Mn catalysta.

| H2/CO ratios | CO | CO2 | Hydrocarbon distribution, carbon based, mol %b |  |  |  |  |  |  |  |  |  | FTYc, mmolCO·gFe-1·s-1 | C2-4= STYd, | O/Pe ratio |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | conv., % | sel., % | CH4 | C2= | C3= | C4= | C2-4= | C20 | C30 | C40 | C2-40 | C5+ |  | g·kgcat-1·h-1 |  |
| 0.5 | 4.2 | 32.7 | 13.2 | 16.0 | 26.9 | 17.3 | 60.2 | 4.4 | 3.1 | 4.0 | 11.5 | 15.1 | 12.2 | 57.7 | 5.2 |
| 1.0 | 7.1 | 25.2 | 17.0 | 13.6 | 25.2 | 15.6 | 54.4 | 6.0 | 4.1 | 5.1 | 15.2 | 13.3 | 16.9 | 73.0 | 3.6 |
| 3.0 | 11.8 | 17.9 | 29.6 | 10.3 | 19.6 | 10.4 | 40.3 | 9.3 | 6.8 | 5.5 | 21.5 | 8.6 | 13.7 | 43.8 | 1.9 |

a Reaction conditions: 25mg catalyst diluted with SiC (1:3), 533K, 2.0 MPa, GHSV=4000 h-1, TOS= 20h. b The hydrocarbon distribution is normalized on a carbon basis with the exclusion of CO2. c Iron time yield (FTY) = mol of CO converted to hydrocarbons (excluding CO2) per time (s) per weight of iron (g). d STY = space time yield. e olefin/paraffin ratio of C2-4 hydrocarbons.

Table S6

FTO performance during a temperature-scanning experiment at temperatures ranging from 493-613 K over Fe-13Mn catalysta.

| Temp., K | CO | CO2 | Hydrocarbon distribution, carbon based, mol %b |  |  |  |  |  |  |  |  |  | FTYc, molCO·gFe-1·s-1 | C2-4= STYd, | O/Pe ratio |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | conv., % | sel., % | CH4 | C2= | C3= | C4= | C2-4= | C20 | C30 | C40 | C2-40 | C5+ |  | g·kgcat-1·h-1 |  |
| 493 | 6.5 | 10.3 | 11.3 | 6.5 | 11.7 | 7.8 | 26.0 | 3.5 | 2.3 | 2.0 | 7.7 | 54.9 | 19.7 | 40.2 | 3.4 |
| 533 | 10.6 | 24.1 | 19.7 | 11.0 | 20.2 | 10.9 | 42.0 | 6.5 | 4.0 | 2.7 | 13.2 | 25.1 | 27.4 | 91.1 | 3.2 |
| 573 | 20.2 | 37.6 | 28.7 | 9.3 | 21.1 | 10.0 | 40.4 | 9.4 | 4.5 | 2.7 | 16.6 | 14.3 | 42.8 | 137.2 | 2.4 |
| 613 | 42.1 | 47.6 | 33.6 | 5.4 | 21.1 | 8.3 | 34.8 | 15.5 | 6.5 | 2.8 | 24.7 | 6.9 | 75.1 | 207.0 | 1.4 |

a Reaction conditions: 25mg catalyst diluted with SiC (1:3), H2/CO = 1.0, 2.0 MPa, GHSV=4000 h-1, holding time at each temperature: 5h. b The hydrocarbon distribution is normalized on a carbon basis with the exclusion of CO2. c Iron time yield (FTY) = mol of CO converted to hydrocarbons (excluding CO2) per time (s) per weight of iron (g). d STY = space time yield. e olefin/paraffin ratio of C2-4 hydrocarbons.

Fig. S1.

Fig. S1. Total area of H2 consumption as a function of Mn loading from TPR experiments

Fig. S2.

Fig. S2. Iron-time-yield (FTY), product distribution and C2=-C4= olefin space-time-yield (STY) at different H2/CO ratios (0.5, 1, 3) in syngas over a Fe-13Mn catalyst. Reaction conditions: 25mg catalyst diluted with SiC (1:3), 533K, 2.0 MPa, GHSV=4000 h-1, TOS= 20h, syngas composition (%, v/v, H2/CO/N2) = 30/60/10, 45/45/10, 60/20/20.

Fig. S3.

Fig. S3. Iron-time-yield (FTY), product distribution and C2=-C4= olefin space-time-yield (STY) during a temperature-scanning experiment in the range 493-613K over a Fe-13Mn catalyst. Reaction conditions: 25mg catalyst diluted with SiC (1:3), 2.0 MPa, GHSV=4000 h-1, TOS= 20h, H2/CO=1.

Mössbauer spectroscopy is a powerful technique for the identification and quantification of iron-based materials, especially for distinguishing poorly crystallized, microcrystalline, or amorphous phases [S1, S2]. From the spectra (Fig.9, Table S1), the spent Fe-0Mn could be fitted to two outermost sextets corresponding to Fe3O4 and three inner sextets, χ-Fe5C2 (I), ε-Fe2C and χ-Fe5C2 (II), respectively. The two outermost sextets with isomer shift (IS) of 0.28, 0.67 mm/s were assigned to high-spin Fe3+ on tetrahedral sites (A-site) and a mixture of Fe2+ and Fe3+ on octahedral sites (B-site), denoted as Fe3O4 (A) and Fe3O4 (B) [S3]. The fitted sextets with the hyperfine field (Hhf) of 213-217 and 109-111 kOe are attributed to χ-Fe5C2 [S4, S5], and the IS of 0.17-0.23 mm/s, Hhf of 176-187 kOe imply the presence of ε-Fe2C [S5, S6]. For Fe-13Mn, only the Fe3O4 (B) (IS = 0.42 mm/s) exists, indicating that Mn2+ may preferentially substitute the tetrahedral sites in Mn-doped ferrite. Besides, the quadrupole doublet with IS of 0.28 mm/s and quadruple splitting (QS) of 1.03 mm/s is related to the superparamagnetic (spm) Fe3+ [S7]. Particularly, Fe-31Mn consists of two outer sextets assigned to χ-Fe5C2, ε-Fe2C and two inner doublets assigned to Fe3+(spm), Fe2+(spm). Large particles of Fe3O4 are wholly disappeared, carbide content drops sharply to 43.3% and the spm Fe2+/Fe3+ with small crystalline sizes prevail among iron species, probably due to the distortion and carburization restraining effect induced by Mn [S7].

References

[S1] K. Xu, B. Sun, J. Lin, W. Wen, Y. Pei, S. Yan, M. Qiao, X. Zhang, B. Zong, ε-iron carbide as a low-temperature Fischer-Tropsch synthesis catalyst, Nat. Commun. 5 (2014) 5783.

[S2] X.W. Liu, S. Zhao, Y. Meng, Q. Peng, A.K. Dearden, C.F. Huo, Y. Yang, Y.W. Li, X.D. Wen, Mössbauer spectroscopy of iron carbides: From prediction to experimental confirmation, Sci. Rep. 6 (2016) 26184.

[S3] S.K. Banerjee, W. O'Reilly, C.E. Johnson, Mössbauer-effect measurements in feti spinels with local disorder, J. Appl. Phys. 38 (1967) 1289-1290.

[S4] N.K. Jaggi, L.H. Schwartz, J.B. Butti, H. Papp, M. Baerns, Phase characterization of iron/manganese Fischer-Tropsch catalysts: Effect of compositon and reduction conditions, Appl. Catal. 13 (1985) 347-361.

[S5] D.H. Chun, J.C. Park, S.Y. Hong, J.T. Lim, C.S. Kim, H.-T. Lee, J.-I. Yang, S. Hong, H. Jung, Highly selective iron-based Fischer-Tropsch catalysts activated by CO2-containing syngas, J. Catal. 317 (2014) 135-143.

[S6] J.-B. Li, H.-F. Ma, H.-T. Zhang, Q.-W. Sun, W.-Y. Ying, D.-Y. Fang, Comparison of FeMn, FeMnNa and FeMnK catalysts for the preparation of light olefins from syngas, Acta Physico-Chimica Sinica 30 (2014) 1932-1940.

[S7] Z. Tao, Y. Yang, C. Zhang, T. Li, M. Ding, H. Xiang, Y. Li, Study of manganese promoter on a precipitated iron-based catalyst for Fischer-Tropsch synthesis, J. Nat. Gas Chem. 16 (2007) 278-285.